Window and Door U-value testing

at the National Physical Laboratory (NPL)

Apparatus used						NPL Wall Guarded Hot Box

NPL Rotatable Hot Box

Window & Door measurement standard			BS EN ISO 12567-1:2000

Cost of standard window measurement 			£1900 + VAT

Cost of standard door measurement			£2000 + VAT

# Window size used for testing

In principle any size up to 1800 mm x 1800 mm could be measured but in practice one of the two sizes shown below should be selected:

Size 1		(1198 ( 2 mm high) x (1198  ( 2 mm wide) x max thickness of 150 mm

Size 2		(1478 ( 2 mm high) x (1228  ( 2 mm wide) x max thickness of 150 mm

This is the FENSA standard size.

Window designs used for testing

In principle any design can be measured. The design should be chosen to be representative of the window type of interest. To show compliance with Building Regulations and for comparison purposes, however, the following designs have been selected by the Glass and Glazing Federation in their document: “Section 2 – Window and Door System U-values: Provision of certified U-values” and these designs should normally be selected.

Fig. A                                                                               Fig. B

Figure A: Reference window design, Approved Document L1

Figure B. Reference window design, Approved Document L2.

Alternative design

Where the arrangement in Figure A, cannot be accommodated by the system parameters, a central transom may replace the mullion. There would then be a top hung casement over a fixed light.

ADDITIONAL DESIGN DETAILS

Trickle ventilators

There are no rules about whether you test with or without trickle ventilators – its up to you.

## Sills

Normally we test windows without the sill being fitted. But again it is your choice as long as the sill is less than 150 mm deep

INFORMATION THAT IS REQUIRED IN THE TEST REPORT

There are two question sheets at the end of this document – one for a door and one for a window. You should fill the appropriate one out for each system we test.  The measurement standard BS EN ISO 12567-1:2000 requires that we include a cross section drawing of the most important frame profiles giving the main dimensions. We there need you to supply such a drawing (A4 size) for each profile type. That drawing should be an original (not faxed) because it will be included in the Report.

## TEST DETAILS

The window is mounted in a holder panel of expanded polystyrene using “duct tape” to keep it in place. This ensures we do not affect the thermal performance by the fixings. This is shown in the sketch below.

DETAILS FOR DOORS

DETAILS FOR WINDOWS

Ray Williams                     12th March 2002

# Text boxes

1.48 m

1.23 m

1.23 m

Expanded polystyrene holder panel 150 mm thick